# Resolving gel solution

# for 10 SDS-PAGE (18.5 cm  20 cm gels)

For unknown proteins, a 10 gel is an excellent choice for initial characterization.

Use BIO-RAD, IPG Conversion Kit. This Kit allows 18.5 cm wide  20 cm long gels to be run on BIO-RAD’s PROTEAN II xi Cell thus accomodating commercially available immobilized pH gradient gel strips for 2-D second dimension protein separation.

Clean the glass with ethanol and water. Assemble the set: insert a longer glass plate into a slot of clamps; place the spacers and insert a shorter inner glass plate; adjust the plates and spacers (the alignment card could be used for this purpose) so, that spacers and plates are flush at the bottom; tighten clamp screws and place ‘sandwich’ into a casting stand.

Prepare: the flask with rubber stopper and box with ice. Keep a flask on ice during the preparation of solution.

For the gels of 1 mm thickness:

|  | 80 ml (2 gels) | 40 ml (1 gel) |
| --- | --- | --- |
| Acrylamide/Bis-acrylamide (stock solution 30, w/v; crosslinker ratio 29:1; BIO-RAD, Cat.No: 161-0156) | 26.64 ml | 13.32 ml |
| TRIS-HCl 3M, pH 8.8 (0.372 M final) | 9.92 ml | 4.96 ml |
| Glycerol 50 (5 final) | 8 ml | 4 ml |
| Distilled H2O | 34.64 ml | 17.32 ml |
| SDS 10 (0.1 final) | 800 microl | 400 microl |

Degas under vacuum for 15 min (do not forget to keep the flask with solution on ice). Then add:

| TEMED (N,N,N,N’-Tetra-methylethylenediamine; BIO-RAD, Cat.No. 161-0800) | 80 microl | 40 microl |
| --- | --- | --- |
| Ammonium persulfate 10, w/v (0.01 final) | 106.4 microl | 53.2 microl |

Fill the gel cassette with resolving gel solution and put some of iso-butanol on the top of the gel. After polymerization (at least after 30 min) aspirate an iso-butanol from the gel (use a syringe) or wash it with distilled water and fill the gel cassette with stacking gel solution.

Solutions: Tris T-1378 ‘Sigma’ 36.33g/100ml H2O, pH 8.8 with HCl

2002 Julius